[image: ]
 (
PROFICIENCY TESTING SCHEMES:
INTERLABORATORY TEST ON ADHESIVES FOR CERAMIC TILES
 
1
8
th
 ROUND
)

[image: Sigla CEPROCIM_2008][image: Laur_65_FOUNDED_eng]





GUIDELINES


GENERAL INFORMATION
	The ILC scheme named “Interlaboratory tests on adhesives for ceramic tiles” meets the requirements of the standard EN ISO/IEC 17043 “Conformity assessment - General requirements for the competence of proficiency testing providers”. Participation is confidential and each laboratory receives a unique code every year.
 	After completing the statistical calculations of the results, each participant receives a General Report which contains the evaluation of the results based on the “z”-score.
	The adhesive samples provided to participants by CEPROCIM S.A. must be processed by ALL participants between 2 and 13 November 2026, taking into account the following indications:
· the adhesive must be used on the same day the container is opened;
· before performing the tests, the total quantity of adhesive enclosed in the container must be homogenized in order to better disperse the components of the adhesive that may have segregated over time during transport.

INFORMATION REGARDING THE TESTS
	All participants in the scheme will use the adhesive received in the package. The ceramic tiles and the concrete slabs used will be the ones specific to each participating laboratory.
	The tests included in the scheme are:
· initial adhesion strength;
· tensile adhesion strength after water immersion;
· tensile adhesion strength after heat ageing;
· tensile adhesion strength after freeze–thaw cycle;
· open-time after not less than 20 minutes; 
according to EN 12004-2:2017 on cementitious adhesives.
	The amount of water required for preparing the adhesive: 320 ml/ 1 kg adhesive.
	Allow the adhesive to mature for 5 minutes, then mix for an additional 15 seconds.
	The results will be quoted to the nearest 0.1 N/mm2 according to EN 12004-2:2017. The failure pattern will be determined according to Annex B of EN 12004-2:2017.
	The test results must be filled out in the RESULTS FORM and sent by e-mail to CEPROCIM S.A. no later than 15th January 2027.

	


CONTACT:
Technical Manager - Cristina STANCU, cristina.stancu@ceprocim.ro

NOTE: In order to update the database with your organisation’s name, address, phone and fax number, e-mail, internet address, laboratory manager etc., please fill out your data in the empty spaces.



					     
	Organisation name:
	

	Address:
	

	Phone
	
	Fax:
	

	Internet address: 
	http://                                               
	E-mail: 
	






RESULTS FORM



	TEST
	Tensile adhesion strength, N/mm2
	Predominant mode of failure

	INITIAL ADHESION STRENGTH
	
	

	TENSILE ADHESION STRENGTH AFTER HEAT AGEING
	
	

	TENSILE ADHESION STRENGTH AFTER WATER IMMERSION
	
	

	TENSILE ADHESION STRENGTH AFTER FREEZE–THAW CYCLE
	
	

	OPEN TIME AFTER NOT LESS THAN 20 MINUTES
	
	








LABORATORY MANAGER
Name, surname:




NOTE: All participants must process the sample between 2 and 13 November 2026.


CEPROCIM S.A.
#6 BLVD. PRECIZIEI; #6 SECTOR, 062203 POSTAL CODE, BUCHAREST, ROMANIA
e-mail:  office@ceprocim.ro, cristina.stancu@ceprocim.ro; web: www.ceprocim.ro
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